## Slide 1: EECS 598: Literature Review
Ali Besharatian
March 16, 2008

## Slide 2: First Paper
A HARPSS Polysilicon Vibrating Ring Gyroscope
Farrokh Ayazi and Khalil Najafi
University of Michigan
2001

## Slide 3: What is a Gyroscope?
A gyroscope is a device for measuring or maintaining orientation,
It senses angular velocity,
Based on principles of conservation of angular momentum.
A macroscale gyro is essentially a spinning wheel or disk whose axle is free to take any orientation.
A gyroscope in operation with freedom in all three axes. The rotor will maintain its spin axis direction regardless of the orientation of the outer frame.
Foucault Pendulum, a device demonstrating the effect of the Earth's rotation, by rotating 360o in its plane, every 24 hours: This is because plane of the pendulum's swing, like a gyroscope, tends to keep a fixed direction in space, while the Earth rotates under it.

## Slide 4: MEMS Ring Gyros
No Moving parts! (It doesn’t rotate!)
Based on the same principle: conversion of angular momentum.
Applications:
  Traction control,
  Ride stabilization,
  Roll-over detection,
  Digital camera stabilization
  Automotive applications (bias stability of 0.5 deg/s)
  Guidance of missiles (improved performance)
Coriolis Force (the same as Foucault Pendulum) is generated in case of rotation.
Fully Silicon Ring Gyro
The 1st MEMS Ring Gyro (Electroplated Nickel on Silicon)

## Slide 5: MEMS Ring Gyros: Principle of Operation
Forced resonance by drive electrodes
In case of angular momentum,
  Coriolis force transfers energy from primary mode to secondary flexural mode
  This causes secondary resonance in another axis (usually 45o apart)
  Can be sensed by change in capacitance
Advantages are:
  Symmetry
  Vertical Capacitors => Very large
  Sensitivity is amplified by Q
  Low temperature sensitivity (both modes experience the same expansion)
  Ease of control and compensation: electronic tuning
The drawback is small effective mass
Anchor
Anchor
Sense mode
Drive mode
Eight Springs:
Symmetric with 2 identical elliptical resonance modes

## Slide 6: Capacitive read-out
Concept: Change in capacitance based on change in gap, overlap or both.
Here: Change in gap for vertical electrodes.
Parasitic capacitance is the drawback.
To reduce the electronic noise floor:
  Reduce the gap
  Increase the height and radius
  Increase Q
  Reduce wo, but keep it
    beyond env. interferences
    and below Brownian noise floor
  Minimize the input referred noise of the interface circuit
  Increase the drive amplitude (qd)
    But only below nonlinear effects
  Increase the polarization voltage
Should be maximized
Should be minimized

## Slide 7: Estimated/Simulated Parameters
Resonant Frequency
Material Quality Factor:
M = Effective Mass
D = Damping Coefficient
k = Spring Constant

## Slide 8: Fabrication Process (HARPSS)
High Aspect Ratio combined Poly and Single Crystal Silicon
A combination of BULK and SURFACE micromachining
Steps:
  Deep Boron Doping (P++)
  Deep Etching (20:1 – 80um)
  Trench Refill
    Oxide Deposition
    Poly-Silicon Deposition
  Metallization
  EDP Etch
  Sacrificial Oxide Etch (Release)

## Slide 9: Advantages
Single wafer
  Simpler than Nickel gyro (i.e. electroplated)
  No bonding
Stress Cancelation by touching Poly-Silicon films
Fully Silicon
  Low TCE mismatch,
  No bonding
Poly-Si springs:
  High Q (Cos4q mismatch is caused by crystal asymmetry of SC Si.)
  Orientation independent
Better material properties than Ni (higher Q)
Tall structures (100s of um):
  Large capacitances for measurement
By changing the oxide thickness, the gap can be controlled easily from sub- to 10s of um.
  Large capacitances for measurement

## Slide 10: Challenges
Void in poly-silicon trench refill process can be a source of energy loss (lower Q)
Excessive undercut of the Si substrate may cause the be soft and dissipates more energy.
voids

## Slide 11: Compensation (Tuning)
By applying a CMOS level DC voltage the degenerate frequency can be canceled:
  0.9V at 22.5o axis
  0 at 45o axis
  (this would be 15.5V for the Ni gyro)

## Slide 12: Test Results
Vacuum (1mTorr)
  Q = 6000 (lower due to voids)
  Modification in etch/refill process increases Q to 10000-20000 range. (up to 85000)
Open Loop (low vac – off chip circuit):
  Q = 250 (poor vacuum – 10 times reduce)
  Measured Capacitance: 500fF
  Parasitic Capacitance: 2pF (output affected by 4 times)
  Drive Amp: 150nm
  200uV/deg/sec
  Resolution <1deg/s (BW: 1Hz)
  Limitation: Ckt Noise
  Dynamic range: ±250deg/sec (BW: 5Hz)
Future Work:
  Parasitic Capacitance Elimination
  0.01 deg/s/(Hz)0.5 for next generations

## Slide 13: Second Paper
Batch-Processed Vacuum-Sealed Capacitive Pressure Sensors
Abhijeet Chavan and Kensal D. Wise
University of Michigan
2001

## Slide 14: General Device Info.
Capacitive sensing (~2pF change)
  Advantages:
    High Pressure Sensitivity
    Low Temperature Sensitivity
    Low Power
Vac. sealed ref. cavity:
  Lower trapped gas effects
  Wider BW (low damping)
  No Stiction
Applications:
  Automotive,
  Environmental
  Medical
  Industrial Proc. Control
  Distributed Weather Forecasting Networks
Different curves for different operating points
500-800Torr
Res: 25mTorr (1ft!)
Diameter:
920-1100um
~3um
~10um
Tensile Stress (~25MPa)

## Slide 15: Barometric Pressure Sensors
Two fabricated devices:
  Single lead (metal on glass)
  Multiple leads (better parasitic cancelation)
Barometric (absolute) pressure sensors.
Both hermetically sealed with Poly-Si / Glass bonding
Poly is used for lead transfer

## Slide 16: Fabrication Process
DWP Process
Anodically bonded to a glass wafer.
Std. CMOS - Wafer Level!
Fully integrated ckt possible!
Single Lead Detail:
  8 masks:
  Recess Etching (KOH)
  P++ Boron Doping
  ONO Deposition
  Poly-Si Deposition and lightly doping (lower temp)
  Optional CMP
  Metal Connections (lift-off)
  Metal On the glass
  Anodic Bonding
  EDP Release
  Optional parylene coating
Since the bonding is done in vacuum, membrane is deflected upon release.
  Single Lead
  Multiple Leads

## Slide 17: Multi Lead Device
2 levels of poly
Leads: between second poly and glass
Ti/Pt on glass getters out diffusing oxygen.
Leak rate < 1.1e-8 atm.cm3/s
Lead Transfer: Glass electrode / poly1/poly2 / poly1/external-metal
Poly ring is isolated => tests needed to verify.

## Slide 18: Switched Capacitor Sensing
CS and CF can exchange their roles: output will be inversely proportional to CS, resulting in linear measurement!

## Slide 19: Test Results
 |  |  | Single Lead | Multi Lead
Sensitivity (fF/torr) |  |  | 27 | 39
TCO (ppm/oC) |  |  | 3969 | 1350
TCS (ppm/oC) |  |  | 1000 | 1000
Resistivity (ohms) |  |  | 46 – 100 | 50
TCO (ppm/oC) |  |  | 1200 - 1600 | ?
Parasitic Cap. (%) |  |  | 25-50 | 5
Resolution (mtorr) |  |  | 25 | 25
Range | (torr/sensor) |  | 50 | 50
 | Total |  | 3.5V/5V | ?
Resolution Needed (bits) |  |  | 12 | 12
Residual Pressure (mtorr) |  |  | <200 | ?
Durability (2 years) |  | Co | ? | -22 fF
 |  | Sensitivity | ? | 30-50 ppm/mmHg
 |  | Offset | ? | -800 ppm/year
TCO: thermal coefficient of Offset
TCS: Thermal Coefficient of Sensitivity
Co = 12pF
Single Lead
Multi Lead

## Slide 20
Thanks for Your Attention!
Questions?